## Slide 1: Cargo hold coating performance analysis
Data and Performance Pictures
Victor wang
Oct. 2019

## Slide 2: Background & Purpose
Evaluate the in-service performance of the Jotaguard Series and support the SAR &Marketing

## Slide 3: Background
Jotaguard 600 Series
630,660,690,690S
Jotamastic Series
80,87,90
Jotacote Universal
Jotaprime 500
Penguard FC
Primastic
Others
Ultra Premium
Premium
Qualified
Standard
Commercial
Strengthen the strengths
Convince the customers to use the ultra premiums

## Slide 4: Purpose
Product analysis
Marketing positioning
Sales focus
Internal factors
R&D formula
Company strategy
Product application
Customer preference
Voyager lines
External factors
Competitor product innovation
Industry cycle
Controllable
Uncontrollable
Start

## Slide 5: 数据挖掘和收集
Sup porting text here.
When you copy & paste, choose "keep text only" option.
0 2

## Slide 6: Product sales reference
NB
DD
Projects No.
Sales Volume
Main Focus
DD sales is increasing steadily while NB is decreasing generally.
The No. of projects decreasing with the volumes going up, it indicates single project is getting larger. More larger vessel size is using the Jotaguard series.

## Slide 7: Customer Profile
NB
Notes: 点击图像可播放

## Slide 8: Customer Profile
DD
Notes: 点击图像可播放

## Slide 9
1%
JOTAGUARD 690S
3%
JOTAGUARD 690
36%
JOTAGUARD 660
61%
JOTAGUARD 630
Top 10 Customer Preference(product composition)
Opportunity
1. Jotaguard 630&660 is the main product used, maintain the volume and improve the volume of the more profitable 690&690s.

## Slide 10: Top 10 Customer Preference
Invoiced Customer Name (top10) | Volume
Sinopacific Shipbuilding Group Co., Ltd. | 991305
CSSC Complete Equipment&Logistics Co., Ltd.-SWS | 808720
KANSAI PAINT MARINE CO., LTD | 740320
China National Shipbuilding Equipment&Materials (East China) Co., Ltd.-JN2# | 615160
Tianjin Xingang Shipbuilding Heavy Industry Co., Ltd. | 450080
Jiangsu New Times Shipbuilding Co., Ltd. | 431280
MARAN DRY MANAGEMENT INC | 421260
OLDENDORFF CARRIERS GMBH & CO.KG | 414660
COSCO Shipping Heavy Industry (Zhoushan) Co., Ltd.-NB East | 410160
COSCO Shipping Heavy Industry (Yangzhou) Co., Ltd. | 389632
1. Only KANSAI PAINT MARINE CO., LTD, OLDENDORFF CARRIERS GMBH & CO.KG
used Jotaguard 690&690s
2. In our research, the main customer to get the performance data is Kansai and oldendorff.

## Slide 11: Analysis process
0 3

## Slide 12: Process of performance analysis
调研和收集
设计调研报告，收集收集数据
数据清洗
Python, Excel清理数据
建模分析
运用统计模型以及市场分析模型分析数据
创建数据库
收集到的数据，公司内部销售数据存入Mysql
可视化报告
Power bi 可视化报告

## Slide 13: Collecting Performance Data

## Slide 14: Rating schema
Rusting
Flaking
Cracking
Scratches
Cargo type
Average voyages
Cleaning time
Detergent liters
Cleaning fees
Rating the values with some standard
AS=100-(100*rusting+50*flaking+10*scratches+80*cracking)
Anticorrosive property
Vessel size
Vessel age
Product type
Other factors
Rating the property with some standard
Cleaning property
Last cargo
People needed
As discussed, the overweight of the anticorrosive should be 60%, the cleaning property should be 40%.
Total performance=60% AS+40% CS

## Slide 15: Product Profile(Jotaguard series)
Jotaguard 690S has the best performance during 3-5 service years
630 is better than 660 after 2 years.
690 is seldom used.
Most vessels will be docked in 3-5 years.

## Slide 16: Product Profile(all including competitors)
Compared to other competitors , jotaguard series has better performance in 3-5 years with cargo type A,B,C,D（all cargo types）
*Diamond shape represents jotaguard

## Slide 17: General comparision
CMP has the highest average performance in the ranking.
Jotaguard series is much better than the Jotun average.
Jotaguard 630,660 performed very well with type D.
Supplier | Product | Main Cargo Type | Average of Performance score
Jotun | Jotaguard 630 | D | 99
Jotun | Jotaguard 660 | D | 99
Jotun | Jotaguard 660 | A,B,D | 98
Jotun | Jotaguard 660 | A,D | 97
Jotun | Jotaguard 690 S | ALL | 97
Jotun | Jotaguard 630 | A,C,D | 93
Jotun | Jotaguard 630 | B,D | 92
Jotun | Jotaguard 660 | C,D | 92
Jotun | Jotaguard 630 | A,B,C | 91
Jotun | Jotaguard 690 S | A | 91
Jotun | Jotaguard 690 S | A,C,D | 91
Jotun | Jotaguard 660 | B,D | 88
Jotun | Jotaguard 690 | D | 88
Jotun | Jotaguard 690 S | B,C,D | 87
Jotun | Jotaguard 630 | C,D | 86.67
Jotun | Jotaguard 630 | B | 86
Jotun | Jotaguard 690 S | B | 86
Jotun | Jotaguard 690 S | A,B,D | 85
Jotun | Jotaguard 630 | A,B | 82.71
Jotun | Jotaguard 630 | A | 81
Jotun | Jotaguard 660 | A,B | 81
Jotun | Jotaguard 630 | B,C,D | 80

## Slide 18: SWOT Analysis
O
S
W
T
S
W
O
T
Good anticorrosive performance with different cargo types especially the jotaguard series.
High price
Higher application standard
690s is vey good but less consumed
CMP has vey strong performance and lower price

## Slide 19: 分析结论
Recommenddations
0 4

## Slide 20: Recommendations
Suggest the customer to use Jotaguard more especially the jotagurd 690s as it has very good performance in cargo hold. With the performance pictures to be used
Recommend the customer if it carried type D often using jotaguard 630&660 as it has the best performance in the scoring.
Kansai & oldendorff preferred to use jotaguard, we can increase the jotaguard 690s sales.

## Slide 21: Thanks
10.2019
Victor wang